© Engineered Science Publisher LLC

Supporting Information

Thermo-Physical Properties of Graphite and Polyethylene Modified Asphalt Concrete

Mushtaq Ahmad1*, Rayeh Nasr Salam Al-Dala'ien2, Salmia Beddu3, Zarina Binti Itam4

Supplementary Results

Table. S1Bitumen Properties

| Test type | Sample | Test standard | Test results | Recommended Specifications |
| --- | --- | --- | --- | --- |
| Penetration test | 1 | AASHTO T49–93 ASTM D5, | 64 | 60–70 |
|  | 2 |  | 67 |  |
| Softening test | 1 | AASHTO T53–92 ASTM 36–89 | 54.7 | 46–56 |
|  | 2 |  | 53 |  |
| Flash & fire | 1 | AASHTO T48 ASTM D92 | 228 and 262 | >232 °C and >246 |
|  | 2 |  |  | >246 |
| Ductility | 1 2 | ASTMD113 | 25 OC > 100cm | >100cm |

Table. S2Properties of course and Fine Aggregate

| Properties | Test standards | Result |
| --- | --- | --- |
| Bulk specific gravity of course granite aggregates | AASHTO T 85–91 ASTM C 127–84 | 2.71 |
| Water absorption of coarse aggregates | AASHTO T 85–91 ASTM C 127–84 | 0.23 % |
| Bulk specific gravity of Fine aggregates | AASHTO T 84–93 ASTM C 128–84 | 2.64 |
| Water absorption of fine aggregates | AASHTO T 84–93 ASTM C 128–84 | 2.49 % |
| Loss angele abrasion test method A,B,C | AASHTO T 96–92 ASTM C 131–81 | 22.6 % 22.3 % 21.01 % |
| Aggregate impact value test (30%max) | BS 812 | 15.80 % |

Table. S3Mix gradation/Sieve Analysis

| Sieve size (mm) | 20 | 14 | 10 | 4.75 | 2.35 | 1.20 | 0.60 | 0.15 | 0.075 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Passing Ratio (% ) Gradation Upper limit Lower Limit | 100 100 100 | 98.70 100 92 | 75 85 70 | 48 65 45 | 37 49 29 | 29 39 18 | 21 26 24 | 17 24 9 | 5 13 3 |

Fig. S1 otted Sieve Gradation

(a)

Fig. S2(a) Specimen after coring

(b)

25mmx50mm

Fig. S2(b) 25mm thick and 50mm diameter specimen