© Engineered Science Publisher LLC

Supporting Materials

# Pyrolysis of Waste Polyolefin’s into Liquid Petrochemicals over Metal Carbonate

Man Vir Singh1

Department of chemistry, Dev Bhoomi Uttarakhand University, Dehradun 248007, India1

Corresponding Author Email: manvir24365@gmail.com, Mob: 8302389668

Table S1 some physical properties of plastics

|  | Name of Plastics | Thermal Properties |  |  |  | Strength |  | Density |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S.no | Chemical name | Tm | Tg | Td | Cte | Tensile | Compressive |  |
|  |  | 0C | 0C | 0C | ppm/0C | psi | Psi | g/cc |
| 9 | LD-PE | 98 115 | -25 | 40 44 | 100 220 | 1200 4550 |  | 0.917 0.932 |
| 10 | HD-PE | 130 137 |  | 79 91 | 59 110 | 3200 4500 | 2700 3600 | 0.952 0.965 |
| 11 | UHMWPE | 125 135 |  | 68 82 | 130 | 5600 |  | 0.940 |
| 13 | PP | 168 175 | -20 | 107 121 | 81 100 | 4500 6000 | 5500 8000 | 0.900 0.910 |
| 14 | PS (polystyrene) Styron |  | 74 105 | 68 96 | 50 83 | 5200 7500 | 12000 13000 | 1.04 1.05 |
| 15 | PVC (polyvinylchloride) |  | 75 105 | 57 82 | 50 100 | 5900 7500 | 8000 13000 | 1.30 1.58 |

Table S2 calorific values of plastics and petroleum

| Chemical name of feedstock material | Calorific values (MJ/kg) |
| --- | --- |
| PE | 46.3 |
| PP | 46.4 |
| PS | 41.4 |
| PVC | 18.0 |
| LPG | 46.1 |
| Petrol | 44.0 |
| Diesel | 43.0 |
| Light fuel oil | 41.9 |
| Heavy fuel oil | 41.1 |

Table S3 Classification of various plastics basis of fuel produced with noncombustible substance

| Plastics | Descriptions | Examples |
| --- | --- | --- |
| Carbon and hydrogen are consisting plastics. | That type of feedstock provides high calorific heat energy and clean exhaust gas. | Thermoplastic (Polyolefin’s and PS) wastes to produce liquid fuel. |
| Oxygen-containing plastics. | Lower calorific value than above (carbon and hydrogen consisting) plastics. | Polyethylene terphthelete, phenolic resin, polyvinyl alcohol, polyoxymethylene. |
| Nitrogen and sulfur-containing plastics. | Nitrogen and sulfur-containing plastic then convert to fuel. Fuel will release some hazardous gasses (NO2, SO2) after combustion. | Nitrogen containing: polyamide, polyurethane, Sulfur containing: polyphenylene sulfide. |
| Fluorine, chlorine and bromine containing plastics. | Hazardous source, will release corrosive flue gas during thermal treatment and combustion. | PVC |

Table S4 Waste thermoplastic allowed as feedstock for good liquid fuel

| Types of plastic | feedstock for petrochemicals |
| --- | --- |
| PE PP PS Poly(methyl methacrylate) Butyl rubber | allowable allowable allowable allowable allowable |
| Acrylonitrile-butadiene-styrene | Allowable but not desirable because get N containing fuel. |
| # Polyvinyl alcohol # Polyoxymethylene | Allowable but not desirable for fuel because the formation of water and alcohol. Allowable but not suitable for fuel because the formation of formaldehyde. |
| PT-ET | It is not desirable for fuel because produce of terephthalic acid and benzoic acid chemicals. |
| Polyurethane Phenol resin | both are not desirable for liquid hydrocarbons fuel |
| Polyvinyl chloride Polyvinylidene chloride | allowable but not desirable because it is provided chlorine containing fuel |

Table S5 Chemical composition of liquid petrochemicals from waste LD-PE and HD-PE and PP with 5% MgCO3

| RT | Name of Compounds | Area % | RSI | RT | Name of Compounds | Area % | RSI |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 4.84 | Cyclobutane, 1-butyl-2-ethyl- | 2.69 | 974 | 12.22 | 1-Dodecanol, 3,7,11-trimethyl- | 0.73 | 927 |
| 4.93 | Decane, 2,5,6-trimethyl- | 1.60 | 939 | 12.32 | 1-Octanol, 2-butyl- | 0.41 | 941 |
| 5.05 | Sulfurous acid, octyl 2-pentyl ester | 0.39 | 919 | 12.52 | 1-Dodecanol, 3,7,11-trimethyl- | 0.57 | 932 |
| 6.14 | 1-Dodecanol, 3,7,11-trimethyl- | 0.90 | 934 | 13.05 | Cyclohexadecane | 3.25 | 979 |
| 6.21 | 1-Dodecanol, 3,7,11-trimethyl- | 0.96 | 951 | 13.10 | Eicosane | 2.71 | 953 |
| 6.35 | 1-Undecene | 3.57 | 977 | 13.29 | Cetene | 0.39 | 979 |
| 6.45 | Oxalic acid, isobutyl nonyl ester | 2.12 | 944 | 14.16 | Heptadecyl trifluoroacetate | 3.09 | 979 |
| 7.47 | Naphthalene, 2-(1,1-dimethylethyl)decahydro-4a-methyl- | 0.78 | 855 | 14.22 | Heptadecane | 2.60 | 975 |
| 7.84 | 1-Dodecene | 3.90 | 973 | 14.39 | 8-Heptadecene | 0.32 | 981 |
| 7.94 | Dodecane | 2.36 | 981 | 14.62 | 1-Dodecanol, 2-hexyl- | 0.78 | 942 |
| 8.01 | 4-Nonene, 3-methyl-, (Z)- | 0.32 | 849 | 14.90 | 2-Hexyl-1-octanol | 0.85 | 938 |
| 9.27 | 1-Tridecene | 4.33 | 986 | 15.26 | Eicosane | 5.23 | 979 |
| 9.36 | Decane, 2,4,6-trimethyl- | 2.53 | 967 | 15.43 | 1-Decanol, 2-hexyl- | 0.52 | 954 |
| 9.47 | 3-Eicosene, (E)- | 1.85 | 929 | 16.26 | Eicosane | 4.98 | 980 |
| 9.57 | Trichloroacetic acid, tridecyl ester | 0.92 | 948 | 17.21 | Eicosane | 4.90 | 991 |
| 9.68 | Hexyl octyl ether | 1.45 | 894 | 18.11 | Heneicosane | 4.11 | 981 |
| 10.00 | 1-Hexadecanol | 0.57 | 951 | 18.97 | Eicosane | 4.11 | 980 |
| 10.60 | 1-Tetradecene | 4.20 | 976 | 19.79 | Eicosane | 3.19 | 981 |
| 10.68 | Tetradecane | 2.22 | 974 | 20.58 | Eicosane | 2.93 | 978 |
| 10.76 | 10-Heneicosene (c,t) | 0.33 | 975 | 21.33 | Eicosane | 2.48 | 967 |
| 11.33 | 1,3,5-Triazine, 1,3,5-tricyclohexylhexahydro- | 0.36 | 943 | 22.07 | 2-methylhexacosane | 2.26 | 963 |
| 11.87 | E-14-Hexadecenal | 3.34 | 975 | 22.83 | 2-methylhexacosane | 1.85 | 963 |
| 11.93 | Pentadecane | 2.00 | 966 | 23.70 | 2-methylhexacosane | 1.45 | 965 |
| 12.00 | 10-Heneicosene (c,t) | 0.31 | 980 | 24.72 | 2-methylhexacosane | 1.13 | 967 |
| 12.12 | 10-Heneicosene (c,t) | 0.37 | 958 | 25.92 | 2-methylhexacosane | 0.76 | 969 |